Speeds and Feeds for 1397,1399, and 1410 series parabolic drills. 130 deg self centering point with 38 deg helix angle. All drills are made from M35 cobalt high speed steel.

Hardness                      Feed Per Rev.

Material                                     Bhn       SFM    1/8”dia     ¼”       3/8”      ½”

| Aluminum 2011,2024,6061,7075 | * | 350 | 0.0040 | 0.0060 | 0.0085 | 0.0110 |
| --- | --- | --- | --- | --- | --- | --- |
| Free Machining 12L14, 1215,11L17 | 80-150 | 120 | 0.0040 | 0.0046 | 0.0070 | 0.0095 |
| Low Carbon Steel 1008, 1018, 1020 | 125-175 | 100 | 0.0030 | 0.0040 | 0.0060 | 0.0080 |
| Medium Carbon Steel 4140, 8620 | 200-280 | 90 | 0.0030 | 0.0040 | 0.0060 | 0.0080 |
| Tool Steel, H.S.S A2,D2,M2,M42 | 300-400 | 65 | 0.0025 | 0.0035 | 0.0055 | 0.0075 |
| Cast Iron | 120-175 | 85 | 0.0030 | 0.0040 | 0.0060 | 0.0080 |
| Stainless Steel 300 Series | 160-200 | 70 | 0.0020 | 0.0032 | 0.0048 | 0.0066 |
| Stainless Steel 400 Series | 180-260 | 55 | 0.0020 | 0.0032 | 0.0048 | 0.0066 |
| Stainless Steel 15-5, 17-4 | 160-200 | 65 | 0.0020 | 0.0032 | 0.0048 | 0.0066 |
| Titanium 6AL-4V | 320-380 | 25 | 0.0018 | 0.0029 | 0.0041 | 0.0060 |
| Inconel 625, 718 | 280-320 | 20 | 0.0010 | 0.0020 | 0.0033 | 0.0045 |
| Copper, Bronze | 120-160 | 80 | 0.0040 | 0.0060 | 0.0085 | 0.0110 |
| Brass (360 half hard) | * | 200 | 0.0040 | 0.0060 | 0.0085 | 0.0110 |

Speeds and feeds are based on bright finish stub or jobber drill.

For taper length drills reduce speeds and feeds by 15%.

TIN coating increase your rpms by 15% from above recommendation

TIALN coating increase your rpms by 25% from above recommendation

PECKING---- first peck after 3X diameter, all other pecks 1-1.5 X diameter

(example. ¼ dia drill in steel, 1st peck after drilling .750 deep, then peck every .300)

for harder materials or gummy materials peck more often

for free maching steels peck less often

6 guidelines for best cutting results

| Use lots of coolant | keep tool concentricity low | Follow pecking guidelines |
| --- | --- | --- |
| workpiece rigidity is important | Use ER or TG style collet chucks | Spot drill for Taper length drills |

Note: Cutting speeds, feeds, and lubrication data are given as starting values only. Parameters should be varied to suite your particular conditions. MariTool is constantly improving products, tolerances, and reliability. As such, these speeds and feeds are subject to change without prior notice. Cutting tools may shatter and or produce dangerous fumes when being used. Appropriate protection is advised.